## Slide 1: Electronic structure of graphene
References:
Orbital Interactions in Chemistry, Chpt. 13 (in Readings list)
Kuno Chpt. 10
P. R. Wallace, Phys. Rev. 1947, vol. 71, p. 662.
Castro Neto et al., Rev. Mod. Phys. 2009, vol. 81, p. 109.
Nanotubes: T. W. Odom et al., J. Phys. Chem. B 2000, vol. 104, p. 2794.

## Slide 2: Electronic structure of graphene and carbon nanotubes
A good description of most real crystals with tight binding requires:
  Extension to 2 or 3 dimensions
  Inclusion of overlap terms (S)
  A multi-orbital basis (multiple atoms and/or multiple atomic orbitals per Bravais lattice site)
The third of these is the most significant: unless basis orbitals are widely separated in energy, the resulting energy bands will include contributions from multiple atomic orbitals.
The “secular determinant”, a result of the variational theorem of quantum mechanics, can be used to find band structures in terms of a small number of parameters, whose values are determined by calculation or experiment.
We’ll look at the band structure of graphene as an example of how this is done.

## Slide 3: The secular determinant: Estimating molecular orbital energies in LCAO approach
Express molecular orbitals as sum of atomic orbitals, each with an appropriate coefficient:
From the Schrodinger equation, MO energies ei are given by:
The numerator and denominator are sums of integrals between each of the possible atomic orbital pairs:
(overlap integral)
(interaction integral)

## Slide 4: The secular determinant: Estimating molecular orbital energies in LCAO approach
Variational result:
The coefficients that minimize the ei’s are found by solving a system of linear equations:
Because this is a system of homogenous linear equations (RHS = 0), the following determinant must be equal to zero:
This “secular determinant” yields a polynomial for ei whose roots give the MO energies
Smm = 1, H and S terms between distant atoms will be negligible, and H12 = H21* etc.
Coefficients can be worked out once ei are known, but often we’re happy with just ei’s
or
or

## Slide 5: Secular determinant: H2 (or ethylene)
Supposing symmetric case (H11=H22=E0):
E – E0
E1
E2
S generally has opposite sign from H
H negative for orbital lobes of same sign

## Slide 6: The secular determinant in a periodic lattice:
In a crystal, we take the same variational approach, but starting with a Bloch function for each atomic orbital.
For example:
Our job is then to find energies Ei for each value of wavevector k using a secular determinant that accounts for interaction integrals (H’s) and overlap integrals (S’s, if used) between each of the atomic orbital Bloch functions. For example
Bloch function for atomic orbitals ɸA located at RA
Bloch function for atomic orbitals ɸB located at RB

## Slide 7: Tight-binding model for graphene:
We simplify the secular determinant by neglecting overlap, and noting HAA = HBB for the two equivalent carbon sites in graphene:
A
A
A
A
A
A
A
B
B
B
B
B
B
B
B
Here, the atomic wavefunction is the same for each carbon atom, but RA and RB describe two different Bravais lattices centered on the two different basis sites in the unit cell.

## Slide 8: Tight-binding model for graphene:
H11:
Interaction integral for members of the same Bravais lattice (or “sublattice”, i.e. A-A or B-B)
a should be bond length

## Slide 9: Tight-binding model for graphene:
H12:
Interaction integral for members of the different Bravais lattices (or “sublattice”, i.e. A-B):
a should be bond length

## Slide 10: Tight-binding model for graphene:
Putting it together:
With a the bond length = 1.42Å

## Slide 11: Tight-binding model for graphene:
Putting it together:

## Slide 12: Tight-binding model for graphene:
Putting it together:
combined
Add overlap S12= -0.1

## Slide 13: ARPES: Angle-resolved photoemission spec.
Cu(111) surface state (hexagonal lattice, 1 electron per site):

## Slide 14: ARPES: Angle-resolved photoemission spec.
Tri-layer epitaxial graphene, near K point:

## Slide 15: Quantum confinement: Carbon nanotubes

## Slide 16: Quantum confinement: Carbon nanotubes: wavefunction must be periodic with roll-up vector

## Slide 17: Quantum confinement: Carbon nanotubes
Bands within Brilloiun zone (depicting unique states) highlighted:
… would be better to plot sub-bands within BZ for 1D unit cell defined by translation vector along tube axis.